## Slide 1: Li- ion modeling physics-based
Dongmyung Suh

## Slide 2: Design of Li ion battery simulation Model
Physics based Li-ion cell model requires considering thermodynamics, mass/charge transfer, electrochemical reaction
Spectral Element Method as numerical method (high numerical accuracy and stability)
Powell hybrid method is applied to solving the system of non-linear algebraic equations.
Simulation should be transient following charging/discharging cycle.
Calculation time step size is self- adjustable.
Post-processing module to analyze calculation results is also needed.
Simulation package will be used freely without the concerns of license fee.

## Slide 3: Li-ion battery (LixC6 | Li yMn2O4)
LixC6 ⇄ x Li+ + x e- + C6
y Li+ + y e- + Mn2O4 ⇄ Li yMn2O4
Negative Electrode
Positive Electrode

## Slide 4: Physics Based Model of Li-ion battery
- in Electrode (Negative/Positive)
as : specific area per unit volume
- Conservation of Charge
- Conservation of Mass
a
b
Li yMn2O4

## Slide 5
- in Electrolyte
- Conservation of Charge
- Conservation of Mass

## Slide 6: Electrochemical Reaction
Butler-Volmer Kinetic Equation
(a) Charging
(a) Discharging

## Slide 7: Spectral Element Method (SEM)
High-Order FEM
Lagrange polynomials as interpolating functions.
Combined with interpolation scheme based on the Gauss-Lobatto-Legendre (GLL) collocation points
High Accuracy, Fast Converging and easy to parallelizing.

## Slide 8
Lagrange Polynomials:
Collocation Points
Roots of Nth order Legendre Polynomials
More densely placed at boundary
Avoid overshooting at boundary
Boundary Condition considered accurately
D (5th Order) =
Differential Equation  Algebraic Equation

## Slide 9: Global Matrix (G ) in SEM
M1 for Element 1
M2 for E 2
M3
M4
M5
=
Spectral elements and collocation points
Matrix Structure for SEM
Assemble each element’s Matrix(M) into a global Matrix (G) using continuity at boundaries between elements

## Slide 10: Solving the system of Non-linear Algebraic Equations
Linear Differential Equations
numpy.linalg.solve(M, Constants)
Non-Linear Differential Equations
scipy.optimize.root( fPM6a, yAll, method="hybr")
Spectral Element Method & Non-linear Solver were implemented in Li-ion simulation code (in Python)

## Slide 11
Negative Electrode:
3 Elements,10th order
Positive Electrode:
5 Elements, 10th order
Electrolyte:
9 Elements, 10th order
particle:
1 Element,
20th order
particle
1 Element,
20th order
Spectral Elements and Nodes
in Li-ion Model (Pseudo 2D)
-
+

## Slide 12: Li-ion battery Simulator & its Postprocessor
Developing the numerical algorithm
Coding simulation & post-processing programs with Python (PyQt5)

## Slide 13: Properties and Parameters
- from Doyle and Newman(1996) Journal of the Electrochemical Society, 143(6), 1890

## Slide 14: Comparison Simulation Results with Experiments
* exp. data from Doyle, M., & Newman, J. (1996). Comparison of the modeling predictions with experimental data from plastic lithium ion cells. Journal of the Electrochemical Society, 143(6), 1890
1C = 17.5 A/m2
Simulating conducted with this model shows a close agreement with test data Doyle & Newman got from Li-Mn2O4 battery cell

## Slide 15: Potential Distribution in Discharging
100% 17.5Ah/m2
Li+
Neg. Electrode
Pos. Electrode
1C-20%
1C-40%
1C-60%
1C-80%
1C-80%
1C-60%
1C-40%
1C-20%
Potential evolution in the cell in discharging at 1C rate

## Slide 16: Potential Distribution in Electrolyte
1C discharging at DOD = 20%
Potential distribution
3C-40%
2C-40%
1C-40%
4C-40%

## Slide 17: Li concentration distribution ( 1C discharging)
Li concentration distribution in Electrode Particles
Li concentration in Electrolyte
DOD= 0%
80%
60%
40%
20%
0%
20%
40%
60%
DOD =80%
20%
40%
60%
80%
0%
(+) Electrode Particle
L- = 175 μm
R+ = 8.5 μm
D+ = 1.0E-13 m2/sec
(-) Electrode Particle
L- = 100 μm
R- = 12.5 μm
D- = 3.9E-14 m2/sec
Del = 7.5E-11 m2/sec in Electrolyte
Surface
Center
Average Li+ con.
In the left figure,
At each DOD condition, Li concentration range is wider in (-) electrode particle than (+) particle.
Along X-direction (the electrode thickness direction), Li concentrations at (+) particle’s surface and center change more than the concentrations of (-) particle.
The reason is because Li ion diffusivity in (-) particle is smaller, but its radius is larger. Also, thickness (L) of (-) electrode is smaller than that of (+) electrode.
Electrochemical reaction rate changes along X-direction(See the next page).
In the right figure,
Li ion concentration distribution in the electrolyte doesn’t much change with depth of discharge(DOD), if it is discharged under the same rate, here 1C
The average concentration of Li in electrolyte is maintained at the initial value, 2kmol/m3.
A
A
B

## Slide 18: Electrochemical Reactions
1C- 80%
1C- 20%
1C- 40%
1C- 60%
Aneg
Apos
Conservation of Charge
A
B

## Slide 19: Li+ transfer in Electrodes, when cell is discharged to Vout = 2.5V
100% 17.5Ah/m2
2C-2.5V
3C-2.5V
1C-2.5V
4C-2.5V
3C-2.5V
1C-2.5V
4C-2.5V
2C-2.5V
X50
X250
As shown in the right figure,
At 1C-2.5V, Li concentration at surface (Csur) has reached its minimum(0) at surface. Due to depletion of Li+, electrochemical reaction is limited and cell output voltage drops quickly.
As discharging get faster than 1C, Csur is higher at Vout=2.5V. But voltage drop quickly by internal resistance.
At higher discharging rate condition, CLi range in the electrode particle,|Csur - Ccen|, becomes wider at both +/- electrodes.
The range of (+)electrode is narrower than that of (-), because the diffusivity and the particle radius of (+) particle are higher and smaller than (-) electrode.

## Slide 20
Left figure shows the Li ion concentration in (+)/(-) particle at x=50 and x=250 position
In (+) electrode particle which has smaller size and higher diffusivity, Li concentration range is smaller than in (-) electrode.
The concentration range expands with higher discharging rate.
The cell’s voltage decreases from 4.2V to 2.5V as it discharges at four different rates. During discharging, Li ions in (-) electrode transfer to (+)electrode.
The difference between Li concentration curves of (+)/(-) electrode is larger at lower C-rate (Max. at 1C). That means more Li ions transfer at slower discharging condition; higher discharge capacity.
In the right figure,
As the discharging rate increases, more Li ion transfer through electrolyte from (-) to (+) electrode. And It causes the concentration gradient of Li ion to increase.
However, the average concentration of Li ion is maintained at the initial concentration, 2 kmol/m3.
-2C-2.5V
-4C-2.5V
-1C-2.5V
-3C-2.5V
-2C-2.5V
-4C-2.5V
-1C-2.5V
-3C-2.5V
Li concentration
in (+) electrode particle(8.5μm) @ X=50
Li concentration
in (-) electrode particle(12.5μm) @ X=250
Li ion concentration in electrolyte at Vout = 2.5V
Average Li+ con.

## Slide 21: Discharging (1/2/3/4C) + Charging (1C)
4Ce
4.1
Charging =1C
Discharging = -1C
Discharging = -2C
-1C
-2C
-3C
-4C
1Ca/4Ca
1Cb
1Cc
1Cd
1Ce
4Cb
4Cc
4Cd
4Ca
1Ca
1Cb
4Cb
4Cc
1Cc
4Cd
1Cd
4Ce
1Ce
Surface
Center
Surface
Center
Charging =1C
Discharging = -1C
Discharging = -4C
During charging/discharging period, Li concentration distribution in the electrode particles widens as shown in the right figures.
Its distribution range shrinks in the relaxation period.
The expansion/shrinkage gets enhanced by increasing discharging rate from 1C to 4C.
At higher discharging rate, the discharging capacity is reduced as well as the charging capacity
The relaxation potential after discharge increases with discharging rate.
2303 sec
2032 sec
1627 sec
1256 sec

## Slide 22: Discharging (1C) + Charging (1/2/3C)
3C_CH
2C_CH
1C_CH
1C_DCH
1C_DCH
3C_CH
2C_CH
1C_CH
763 sec
246 sec
2908 sec
4.2
The charging behavior is simulated at different charging rate.
At higher charging rate,
The cell reaches quickly the charging limit voltage (Vmax = 4.2v) and the charging time is shortened.
But, the amount of Li ions having transferred from cathode to anode electrode is reduced as shown in the right figure.
The discharging capacity will be dwindled.

## Slide 23: Effect of RSEI (SEI resistance)
0.0
0.1
0.2
RSEI (m2) =
The effect of SEI resistance on cell capacity is studied by simulation.
As the solid electrolyte film layer grows, cell’s internal resistance grows.
Cell voltage change at the start of discharge/charge increases with higher SEI resistivity.
As SEI resistivity increases, the time to reach charging limit voltage gets shorter and charging /discharging capacity is reduced..

## Slide 24: Conclusion
Physics based Li-ion cell model is developed successfully.
The model is verified by comparison with test data.
Mass and charge transfer with electrochemical reactions are well analyzed.
The simulation model will be applied to analyzing cell performance issues such as capacity fade and impedance growth.
The simulation tool developed is able to deploy freely to other battery engineers